CSI Format Specification for KUBIT™ railings – with Infill options

Part 1 - General:

  - Section Includes

Pre-engineered KUBIT™ stainless steel Railing System. All drawings, general and

supplementary conditions including division one specifications apply to this section.

  - Related Sections

Division 5: Ornamental Handrails and Railings

1.3	Product References and Design Requirements

1.3.1    Principle items specified in this section are:

a. Stainless steel and Stainless/wood combination handrails.

b. Stainless steel and steel guardrails or other ornamental barrier railings.

c. Stainless steel or tempered-laminated glass infill panels.

d.  Stainless steel perforated, woven or welded infill panels.

e.  Resin infill panels.

f.  Stainless steel rail with LED light insert.

1.3.2	Design requirements are based on IBC/IRC and ADA standards:

A  Guardrails and handrails shall meet or exceed all applicable building codes.

b.  Railings shall have high strength stainless steel to comply with structural requirements with an appropriate safety margin.

c.  All internal members shall be stainless steel, aluminum, or nylon to eliminate the possibility of rust.

d.  Prevent galvanic action and other forms of corrosion by insulating metals and other materials from direct contact with incompatible materials.

1.3.3	Work Included

Provide all materials, labor and equipment necessary to fabricate and completely install 		handrails, guardrails, infill panels, and other railing options as shown on drawings or 			specific herein.

1.3.4	Definitions

Terms and definitions from ASTM E985 and ISO/TC 59 for railing related items apply to 	this section.

1.4	System Performance Requirements

1.4.1	Railings shall meet or exceed the requirements of all applicable building codes.

1.4.2	Railings shall have high strength stainless steel in order to comply with 1.4.1 with 			adequate safety margin.

1.4.3	All internal members shall be stainless steel, nylon, aluminum, or wood to eliminate the possibility of rust.

1.4.4	Prevent galvanic action and other forms of corrosion by insulating metals and other 			materials from direct contact with incompatible materials.

  - Submittals

    - Shop Drawings for architectural approval, showing fabrication and installation of 	handrails and railings including plans, elevations, sections, details of components and

attachments to other units of work.

    - Product data for stainless steel/wood products to be supplied by the manufacturer.

    - Structural computations or test data/evaluations, material properties, PE (professional

engineering) calculations signed/sealed in the State of the project, and other information needed to ensure satisfactory structural compliance to applicable building codes to be supplied by the manufacture, based on final fabrication drawings and documents.

    - Maintenance instructions: Provide manufacturer‘s maintenance and cleaning

instructions.

    - Warranty: Provide manufacturer‘s warranty effective from completion of work.

    - Initial selection

Provide 6“ long handrail samples complete with supports and rosette covers to

demonstrate stainless steel grade and finish.

    - Final verification

Qualification data for authorized installers specified in Quality Assurance is to

demonstrate their capabilities and experience. Include list of completed projects with 	project and architect names.

  - Quality Assurance

    - Single Source Responsibility: Materials shall be supplied by HDI Railing Systems, 3905 	Continental Drive, Columbia PA 17512 (Tel: 717-285-4088 Fax 717-285-5083).

Regionally based employees installers throughout the U.S. and Internationally.

    - Execution tolerance plus/minus 5/64” (2 mm).

  - Storage

1.7.1    Store handrails and railing systems in a clean, dry location, away from uncured concrete 		and masonry, protected against damage of any kind.

1.7.2	Materials must be kept in their original packaging until installation.

1.8       Project Conditions

1.8.1	All measurements for handrails and railings should be taken from construction site 			elements to which railings are to fasten. This information is to be recorded on final shop 		drawings.

1.8.2	Coordinate fabrication schedule with construction progress to avoid delay of work.

Part 2 - Product:

  - Manufacturer

    - Mechanically fastened Stainless steel railing systems

Manufacturer shall be HDI Railing Systems, a U.S. manufacturer of a custom pre-	engineered, mechanically fastened guardrail and handrail systems, in strict compliance 	with all technical requirements of the drawings and specifications. Miscellaneous metal 	fabricators/suppliers will not be acceptable. This standard is based on HDI Railing 	Systems, 3905 Continental Drive, Columbia PA 17512 (Tel. 717.285.4088 Fax. 	717.285.5083).

2.1.2	Substitutions:  Not permitted.

2.2       Materials for Guardrails and Handrail System

2.2.1	All rails and other tubular components shall be constructed using the following:

2.2.1.1	 Stainless steel grade AISI, type 304/304L or 316/316L; surface to be 240 			grain/grit finish; tubes 1-1/2” (38mm) outside diameter by . 5/64” (2 mm) wall 			thickness.

        - Optional natural wood handrails and top rails to be secured to posts using stainless steel saddles on top of posts: Mitered joints required by changes in direction require stainless steel true bar to be inserted into the underside of the wood. Standard wood types are available in natural beech, birch or maple, other wood types available upon request. All custom stains are subject to customer approval and require customer samples. Wood to be continuous throughout. Returns to wall or floor that require stainless steel bends should have transitions that are smooth and without burrs.

2.2.2	All posts and other components shall be constructed using the following:

2.2.2.1 Stainless steel grade AISI type 304/304L or 316/316L, surface to be 240 			grain/grit finish; posts to be 2“ (50.8mm) x 1/2“ (12.7mm) rectangular bar , finish

and final design to be strictly in accordance with KUBIT design guidelines.

2.2.2.2  Stainless steel grade AISI type 304/304L or 316/316L, surface to be 240 			grain/grit finish barrel fittings including handrail attachment support and post 			attachment components strictly in accordancce with KUBIT™ design 				guidelines.

.

2.2.2.3	  Fastening bolts to be stainless steel or other high strength material as 				determined by engineering requirements.

2.2.2.4  Powder coated options available upon request.

    - Fastening bolts to be stainless steel or other high strength material as determined by 	engineering requirements.

    - Infill Panel attachment to be either Pressure Clamps or Panel holders through bolted to 	infill. These are mounted to post using a “Glass Link” bar, offsetting the glass from the 	posts. Infill panel thickness can be 1/2” (12.7mm) or greater as specified. Panel holder

heights are adjustable vertically in accordance with approved drawings (location can be adjusted on site). Vertical distance between panel 	holders must be less than or equal to 25-5/8” (600 mm).

2.3       Glass products, glazing and infill materials

    - Tempered glass:  Provide fully tempered safety glass with polished edges and dubbed 	(blunt) corners complying with ASTM C1048.  Kind FT (fully tempered), condition A (un-	coated).  Types 1 (transparent glass, flat), quality Q3 (glazing select), class, thickness 	and manufacturing process as indicated below. Tempered-laminated glass infill panels 	are required in railings where there is access to areas below the railing (check local 	codes).

2.3.2	Clear glass: Class 1 clear

2.3.3	Tinted glass: Class 2 (tinted heat absorbing and light reducing). Manufacturer’s standard tint color or custom color as indicated below:

a.	Bronze, Gray, or other as indicated

b.	Low iron

c.	Custom pattern, art glass, etch, edges or surface, laminate or embeds, as specified herein.

    - Allowable thickness 9/16" (14.28 mm) to be noted on final shop drawings.

    - Laminated Interlayer: PVB for interior applications; SGP for exterior applications

    - Manufacturing process: Manufacture fully tempered glass by horizontal (roller hearth) 	process with roll wave distortion parallel with bottom edge of glass as installed.

2.4	Stainless perforated, woven or welded metal infill panels

    - Perforated metal infill panels

Stainless steel perforated metal infill panels with continuous frame by HDI Railing Systems. Installed post centers are required complete with sketch, to allow panel fabrication. Standard pattern to be 3/8“ (9.5 mm) square holes on ½“ (12.7mm) straight row centers or 3/8“(9.5mm) round holes on ½“ (12.7mm) staggered centers surrounded by a continuous 1/2“ (12.7 mm) x 1.5“ (38 mm) 304 SS rectangular tube frame with hairline joints. Grain is 240 grit and polished longitudinally to the miter cuts.

    - Woven or welded metal infill panels

Stainless steel woven or welded infill panels with continuous 1/2“ (12.7 mm) x 1.5“ (38 mm) 304 SS rectangular tube frame with hairline joints by HDI Railing Systems. Installed post centers are required complete with sketch, to allow panel fabrication. Finish is brushed and polished.

Manufacturers Panel Design indicated below using Stainless steel bars woven to create a linked pattern, framed with rectangular SS frame:

      - Stainless steel bars formed into rounded shapes woven to create a linked pattern.

      - Stainless steel flat bars woven to create a linked pattern.

      - Stainless steel bars woven into a rectangular pattern.

      - Custom pattern as specified herein.

2.5   Woven Cable Infill Mesh panels

2.5.1	Material:  Stainless steel, AISI 316L; wire rope diameter 1.5mm

spaced with offset sleeves.

2.5.2	Horizontal mesh (standard) with offset sleeves positioned horizontally.

2.5.3	Aperture opening 75 – 80mm measured vertically.

2.5.4	Panel frame 5/8” (16mm) diameter with mitered corners type 304 or type 			316

2.5.5	Woven mesh panels attached to posts with standard attachment bar clamp.

2.6	Resin infill panels – blend of polyester resin for interior applications

2.6.1. 	Panel design: flammability results equivalent to Class A for most panel configurations;

most panels made from 30%-60% recycled content. Manufacturers panel design to be

indicated below:

2.6.1.1   Material options: indicate textiles, botanicals, prints, textures or Pure

colors (Pure Colors have no embed or interlayer; indicate Pantone®

color)

2.6.1.2	 Color: Indicate clear or specify color(s) to accent/contrast with interlayer;

indicate Pantone® color(s) for layers

2.6.1.3   Finish: indicate textured (one or both sides); matte or gloss; indicate

edge finish

2.6.1.4   Embedded material: for three dimensional effect within resin panel:

- indicate embedded material such as fabric, pine needles, glass fragments

- indicate color of embedded material

2.7	LED lighting inserts (LED components subject to change; contact Manufacturer for 	most 	current LED specifications)

2.7.1	Stainless steel rail with LED light strip inserts grade UNS 1.4305, type 304 or type 			316; surface to be # 6 finish (240 grain/grit); tubes 1.5” (38mm) outside diameter by 		.075“ to .090” (1.5 mm – 2.3mm) wall thickness.

2.7.2	LED light strip inserts with a beam spread of 45 degrees to 90 degrees, or 				asymmetrical beam spread of 28 degrees and 65 degrees off nadir. Other beam 			spreads available; contact the manufacturer.

2.7.3	 Standard clear lens; frosted lens optional.

2.7.4	Light output at 42“guard height, lumens per ft as indicated, ranging from 36.8 to 616 			lumens per ft dependent on standard or high output and symmetrical or asymmetrical.

2.7.5	Color temperature as indicated, ranging from 2700K (Kelvin) to 6500K, dependent on 			lumens per ft and beam spread required.

2.7.6	Electrical supply for LED strip inserts to be 120-277Volt supply for 24-volt remote 			power supply. (Power supply range 20-240watts)

2.7.7	Transition sleeves for intermediate supports, backing strips for LED light strips, slotted 			tube inserts and mounting clips by HDI provided as required.

2.7.8	Power supply low voltage dimmers available.

  - HDI Puck LED (LED components subject to change; contact Manufacturer for most current LED specifications)

    - Stainless steel rail with LED puck fixtures grade AISI type 304 or type 316; surface to be #6 brushed finish (240 grain/grit); tubes 1.5“ (38mm) outside diameter by .075“ to .090“ (1.5mm – 2.3mm) wall thickness.

    - Individual LED puck fixtures come in 316 stainless steel grades. 18mm diameter x 24mm depth.

    - LED puck fixtures power consumption is 1.2W per fixture and are powered by DC24V power.  Each fixture is IP67 waterproof rated and have 3M waterproof internal connectors.  Dimmable fixtures available upon request.

    - Standard clear lens

    - Standard beam angle is 60 degrees symmetric, customized beam angles available upon request.  Asymmetric options are available.   Please contact manufacturer.

    - Color temperature as indicated, ranging from 2700K (Kelvin) to 6000K.  Other solid color options are available upon request such as Blue, Green, and Red.

    - Electrical supply for LED puck fixtures to be 120-277Volt supply for 24 volt remote power supply. (Power supply range 20-240 watts)

    - Power supply low voltage dimmers are available.

    - Low voltage wires for use of connecting fixtures inside of the handrail provided by manufacturer.  Installation of wires and puck fixtures are required in the field during installation process (not pre-assembled in HDI factory).  Pre-drilled and tapped holes for fixture mounting into the handrail can also be provided by manufacturer in advance.  For curved or spiral applications, holes are required to be drilled and tapped in the field.  See manufacturer for more information.

2.9	Fasteners

Anchors shall be fabricated from stainless steel or other materials as determined by engineering requirements with capability to sustain, without failure, load imposed within an appropriate safety factor for the specified material, such as steel anchors or concrete.

2.10  Fabrication

2.9.1	Fabricate railing system for compliance with structural requirements of applicable code.

2.9.2	Pre-assemble railings prior to shipping to greatest extent possible to ensure QC.

Disassemble units and pack as appropriate for shipping and handling requirements.  Clearly mark crates and boxes for re-assembly by location and for coordination with shop drawings.

2.9.3	Stainless steel tubing cuts shall be square, without burrs and where exposed, rounded 	to produce smooth rigid and hairline joints.

Part 3 – Execution:

3.1       Examination

3.1.1	Do not begin installation until substrates have been properly prepared.

3.1.2	Verify that reinforcement and anchoring devices are the correct type, have been located correctly, and have been installed properly.

3.1.3	If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

3.2	Preparation

Provide information on fastening point locations for posts where necessary to relevant parties.

3.3	Installation

Installation shall be by HDI Railing Systems or a qualified, authorized representative of the manufacturer. HDI Railing Systems, 3905 Continental Drive, Columbia PA 17512 (Tel: 717-285-4088 Fax 717-285-5083).

    - Installation must be in accordance with standard or non-standard, yet applicable details

(instructions) included on installation/shop drawings provided by HDI Railing Systems.

3.3.2	Install components plumb and in-line, accurately fitted, free from distortion or defects and securely anchored to structure.

3.3.3	Provide anchors, plates, angles, etc., necessary for connecting railings to structure.

3.3.4 	Any and all field welding shall be by a certified welder.

3.3.5	Access for anchors that require through bolting either vertically or horizontally to be made available through General Contractor.

Erection tolerances

    - Maximum variation from plumb shall be 1/4".

    - Maximum offset from true alignment for every 50-foot of railing shall be 1/4", non-	accumulative.

3.4	Cleaning and Protection

    - Remove manufacturer's protective coverings from exposed surfaces after installation.

    - Railings shall be cleaned, including infill panels, by contractor to the satisfaction of the 	owner.

    - Wipe with moistened cloth only.  Do not use cleaning agents with abrasive or 	acid/alkaline content.

    - General contractor to provide protective covering on handrails and guardrails if 	construction is not yet finished in the area where the railings are installed.

  - Correction of deficiencies

All deficiencies in work and/or items not meeting specified requirements shall be corrected in

order to meet specification requirements at no additional cost to owner.

End of Section